## Slide 1: Additive Manufacturing (or 3D Printing) (or Rapid Prototyping) AM methods, and concurrent barriers and challenges
MAE 540

## Slide 2: AM methods
Material extrusion aka Fused Deposition Modeling (FDM): create layers by mechanically extruding molten thermoplastic material (e.g., ABS or PLA, and processing ceramic and metal pastes) onto a substrate.
Price: ~$1000

## Slide 3: AM methods
Powder bed fusion (Direct metal laser sintering, selective laser melting and electron beam melting): use an energy beam (e.g. laser or electron beam) to selectively melt a powder bed.
Price: ~$1000,000

## Slide 4: AM methods
Vat photopolymerization aka stereolithography method (SLA): ultraviolet laser was used to selectively polymerize the UV curable resins to create a layer of solidified material, limited to photopolymers
Price: ~$1000

## Slide 5: AM methods
Direct energy deposition: metallic powder or wire is fed directly into the focal point of an energy beam to create a molten pool
Price: $?

## Slide 6: AM methods
Printing circuits, sensors, and batteries through Direct Write
Panesar et al. (2014) Design Optimization Strategy for Multifunctional 3D Printing

## Slide 7: AM Material Cost
Material Feedstock | Titanium 6AI-4V | Tantalum | Inconel 625 | Stainless Steel 316
Wire—0.035" Diameter (0.9 mm) | $58/lb. | $545.30/lb. | $26.73/lb. | $5.19/lb.
Wire—0.045" Diameter (1.1 mm) | $54/lb. | $545.30/lb. | $23.30/lb. | $4.63/lb.
Wire—0.062" Diameter (1.6 mm) | $50/lb. | $524.88/lb. | $22.17/lb. | $4.57/lb.
Wire—0.093" Diameter (2.4 mm) | $48/lb. | $502.30/lb. | $21.43/lb. | $4.81/lb.
Wire—0.125" Diameter (3.2 mm) | $45/lb. | $438.96/lb. | $21.02/lb. | $4.75/lb.
Wire—0.156" Diameter (4.0 mm) | $44/lb. | $438.96/lb. | N/A | $4.69/lb.
Powder—AM Grade | $120/lb. | $522/lb. | $48/lb. | $10/lb.
http://www.sciaky.com/additive-manufacturing/wire-am-vs-powder-am

## Slide 8: Classification of AM
Classification of additive manufacturing processes by ASTM International (2013)

## Slide 9: Concurrent barriers and challenges
Personal fabrication vs. mass manufacturing
  Suitable products for AM: Customized, low-volume, complex, e.g., aerospace/high-end automotive components, bio-medical products, jewelry, home accessories.

## Slide 10: Concurrent barriers and challenges
Building scalability vs. layer resolution
  Layer resolution for commercially-available AM systems: ~0.1mm (Makerbot Replicator 2) to 25mm
  Full spectrum of build sizes in research
Lee and Kim (2014)
Building nanoscaffolds, nanofilters, nanorobots, and nanoelectrodes with electrospun polymer nanofibers

## Slide 11: Concurrent barriers and challenges
Building scalability vs. layer resolution
  Layer resolution for commercially-available AM systems: ~0.1mm (Makerbot Replicator 2) to 25mm
  Full spectrum of build sizes in research
Daicho et al. (2013) 3D carbon microstructures
Khoshnevis et al. (2006) Mega-scale fabrication

## Slide 12: Concurrent barriers and challenges
Material heterogeneity and structural reliability
  Limited AM materials
  Anisotropic mechanical properties

## Slide 13: Concurrent barriers and challenges
Material heterogeneity and structural reliability
  Functionally-graded materials have uncertain behavior at the material interfaces

## Slide 14: Concurrent barriers and challenges
Use of support material
(a) Build-direction. (b) Subtended angle. (c) Support length. (d) Support volume.
Mirzendehdel et al. (2016)
Effect of support constraint on optimized design

## Slide 15: Concurrent barriers and challenges
Removal of support material
Before etching
After etching
Lefky et al. (2016) Dissolvable metal supports for printed metal parts
(from Dr. Owen Hildreth’s group)

## Slide 16
Gao et al. (2015) The status, challenges, and future of additive manufacturing in engineering

## Slide 17: What’s next?
Geometry design for AM
  3D representations suitable for editing, analyzing and printing
voxel
mesh
LDNI

## Slide 18: What’s next?
Geometry design for AM
  Geometric processing: hollowing and thickening, support generation
  Structure optimization, model validation
  Multi-material representation and analysis
  4D printing, origami sheets
  New design tools: Sketch based, gesture based
  3D optical scanning
  Material-efficient and environment-friendly AM

## Slide 19: 3D marketplaces
Shapeways: Design, Prototype, Buy and Sell custom products; The world's largest online 3D Printing Service, Community and Marketplace.
Thingiverse: Download our files and build them with your lasercutter, 3D printer, or CNC.
Sculpteo: offers everyone rapid online 3D printing services.
Onshape: full-cloud 3D CAD system that lets everyone on a design team simultaneously work together using a web browser, phone or tablet.

## Slide 20: Burr Puzzles and ancient wood joinery
Burr Puzzle: interlocking puzzle consisting of notched sticks, combined to make one three-dimensional, usually symmetrical unit.

## Slide 21: Burr Puzzles and ancient wood joints
Commonly used in architectures in Asian countries

## Slide 22: Burr Puzzles and ancient wood joinery

## Slide 23: 3D printing Burr Puzzles
Song et al. (2015) Printing 3D Objects with Interlocking Parts